Malaysian Journal of Analytical Sciences Vol 24 No 3 (2020): 363 - 372

PHASE BEHAVIOUR STUDY ON MEDIUM-CHAIN TRIGLYCERIDE/ SURFACTANT/WATER SYSTEMS CONTAINING GEMCITABINE

USING PHASE INVERSION COMPOSITION TECHNIQUE

(Kajian Tingkah Laku Fasa Bagi Sistem Trigliserida Rantaian Sederhana/Surfaktan/Air yang Mengandungi Gemcitabine dengan Menggunakan Teknik Komposisi Penyongsangan Fasa)

Nadiatul Atiqah Wahgiman, Norazlinaliza Salim*, Mohd Basyaruddin Abdul Rahman

Integrated Chemical BioPhysics Research, Faculty of Science,

University Putra Malaysia, 43400 UPM Serdang, Selangor, Malaysia

*Corresponding author:  azlinalizas@upm.edu.my

Received: 20 November 2019; Accepted: 21 April 2020; Published:  9 June 2020

Abstract

In this study, the phase behavior of medium-chain triglyceride (MCT)/surfactant/water containing gemcitabine (GEM) was investigated. Ternary phase diagrams (TPD) were constructed with different surfactants (Span 20, Span 60, Span 80, Tween 80) and a mixture of surfactant (Tween 80:Span 80, at ratio 1:1). Two observations were recorded, isotropic and multilayer regions. The isotropic region was classified as a transparent, translucent or homogeneous mixture, while the multilayer region was classified as an opaque, milky or heterogeneous mixture. From the ternary phase diagrams constructed, it showed that MCT/(Tween 80: Span 80, ratio 1:1)/ GEM in deionized water system gave the largest isotropic region with the minimum usage of mixed surfactant, where 25% area of the isotropic region was formed with 1% of the usage of surfactant. The composition of F1 (selection based on the ternary phase diagram) was 0.02 % w/w of GEM, 19.98 % w/w of deionized water, 5.00 % w/w of Tween 80:Span 80 at ratio 1:1 and 75 % w/w of MCT. Nanoemulsion formulation was prepared by low energy emulsification method (i.e. phase inversion composition (PIC) technique). As the formulation was prepared in large scale with PIC technique, sodium chloride solution (0.1 M NaCl solution) was added to form a stable formulation as stabilizer. Effect of different volume of NaCl solution (0.5, 1.0 and 1.5 mL) added into formulation was investigated. The results showed that the particle size increased as the amount of NaCl increased, the effect of the amount of NaCl solution is significant towards particles size on F1. The F1 was stable in normal storage condition as it remained a homogeneous formulation against centrifugation test and it was also stable in storage stability test at different temperature (4, 25 and 45 °C) within three months.

Keywords:  gemcitabine, nanoemulsion, ternary phase diagram

Abstrak

Dalam kajian ini, sifat fasa pada trigliserida rantaian sederhana (MCT)/surfaktan/air yang mengandungi GEM telah dikaji. Gambar rajah fasa ternari (TPD) telah dibina dengan surfaktan yang berbeza (Span 20, Span 60, Span 80, Tween 80) dan campuran surfaktan (Tween 80:Span 80, pada nisbah 1:1). Dua pemerhatian telah direkodkan, rantau isotropik dan pelbagai lapis. Rantau isotropik telah diklasifikasikan sebagai telus, lut atau campuran homogen, manakala rantau pelbagai lapisan telah diklasifikasikan sebagai legap, seperti susu atau campuran heterogen. Daripada gambar rajah fasa ternari yang telah dibina, ianya menunjukkan yang sistem MCT/(Tween 80: Span 80, pada nisbah 1:1)/ GEM dalam air ternyahion telah memberi rantau isotropik yang paling tinggi dengan penggunaan campuran surfaktan yang minimum, di mana 25% keluasan rantau isotropik telah terhasil dengan 1% penggunaan surfaktan. Komposisi F1 (pilihan berdasarkan pada gambar rajah fasa ternari) ialah 0.02% w/w daripada GEM, 19.98% w/w daripada air ternyahion, 5.00% w/w daripada Tween 80:Span 80, pada nisbah 1:1 dan 75% w/w daripada MCT. Formulasi nanoemulsi telah dihasilkan dengan pengemulsi yang rendah tenaga (fasa penyongsangan (PIC). Formulasi yang dihasilkan dalam skala yang besar dengan teknik PIC, natrium klorida (0.1M larutan NaCl) telah ditambah untuk menghasilkan formulasi yang stabil sebagai penstabil. Kesan tiga isipadu larutan NaCl yang berbeza (0.5, 1.0 dan 1.5 mL) telah ditambah dalam formulasi dan dikaji. Keputusan menunjukkan peningkatan saiz zarah apabila jumlah NaCl meningkat, jumlah larutan NaCl memberi kesan yang signifikan terhadap saiz zarah F1. F1 adalah stabil di dalam penyimpanan keadaan biasa apabila ianya kekal homogen ketika diuji dengan ujian emparan dan stabil dalam ujian penyimpanan  kestabilan pada suhu yang berbeza (4, 25 dan 45 °C) selama 3 bulan.

Kata kunci:  gemcitabine, nanoemulsi, gambar rajah fasa ternari

References

- Hayashi, H., Kurata, T. and Nakagawa, K. (2011). Gemcitabine: Efficacy in the treatment of advanced stage nonsquamous non-small cell lung cancer. Clinical Medicine Insights: Oncology, 5: 177-184.

- Alvarellos, M. L., Lamba, J., Sangkuhl, K., Thorn, C. F., Wang, L., Klein, D. J., and Klein T. E. (2014). PharmGKB summary. Pharmacogenetics and Genomics, 24(11): 564-574.

- Toschi, L., and Cappuzzo, F. (2009). Gemcitabine for the treatment of advanced non-small cell lung cancer. OncoTargets and Therapy, 2: 209-217.

- Wang, J., Zhang, X., Cen, Y., Lin, X., and Wu, Q. (2016). Biointerfaces antitumor gemcitabine conjugated micelles from amphiphilic comb-like random copolymers. Colloids and Surfaces B. 146: 707-715.

- Parsian, M., Unsoy, G., Mutlu, P., Yalcin, S., and Tezcaner, A. (2016). Loading of gemcitabine on chitosan magnetic nanoparticles increases the anti-cancer efficacy of the drug. European Journal of Pharmacology, 784: 121-128.

- Salim, N., Basri, M., Abdullah, D. K., and Basri, H. (2011). Phase behaviour, formation and characterization of palm-based esters nanoemulsion formulation containing ibuprofen. Journal of Nanomedicine and Nanotechnology, 2(4): 1-4.

- Mahdi, E. and Sakeena, M. (2011). Effect of surfactant and surfactant blends on pseudoternary phase diagram behavior of newly synthesized palm kernel oil esters. Drug Design, Development and Therapy, 5:311-323.

- Izquierdo, P., Esquena, J., Tadros, T. F., Dederen, J. C., Feng, J., Garcia-Celma, M. J. and Solans, C. (2004). Phase behavior and nano-emulsion formation by the phase inversion temperature method. Langmuir, 20(16): 6594-6598.

- Jaiswal, M., Dudhe, R. and Sharma, P. K. (2015). Nanoemulsion: an advanced mode of drug delivery system. 3 Biotechnology, 5(2):123-127.

- Silva, H. D., Cerqueira, M. A., and Vicente, A. A. (2015). Influence of surfactant and processing conditions in the stability of oil-in-water nanoemulsions. Journal of Food Engineering, 167: 89-98.

- Puglia, C., Rizza, L., Drechsler, M., and Bonina, F. (2010). Nanoemulsions as vehicles for topical administration of glycyrrhetic acid: Characterization and in vitro and in vivo evaluation. Drug Delivery, 17(3): 123-129.

- Koroleva, M. Y., Nagovitsina, T. Y., Bidanov, D. A., and Gorbachevski, O. S. (2016). Nano- and microcapsules as drug-delivery systems. Resource-Efficient Technologies, 2(4):233-239.

- Arbain N. H., Salim N., Masoumi H. R. F, Wong T.W., Basri M., and Rahman M. B. A. (2018). In vitro evaluation of the inhalable quercetin loaded nanoemulsion for pulmonary delivery. Drug Delivery and Translational Research, 67: 497-507.

- Amani, A., York, P., Chrystyn, H., and Clark B. J. (2010). Evaluation of a nanoemulsion-based formulation for respiratory delivery of budesonide by nebulizers. American Pharmaceutical Scientists PharmSciTech, 11(3):1147-1151.

- Samiun, W. S., Ashari, S. E., Salim, N. and Ahmad, S. (2020). Optimization of processing parameters of nanoemulsion containing aripiprazole using response surface methodology. International Journal of Nanomedicine. 15: 1585-1594.

- Asmawi, A. A., Salim, N., Ngan, C. L., Ahmad, H., Malek, E. A., Mas, J. M. and Rahman, A. M. B. (2018). Excipient selection and aerodynamic characterisation of nebulised lipid-based nanoemulsion loaded with docetaxel for lung cancer treatment. Drug Delivery and Translational Research, 9(2):543-554.

- Ribeiro, R. C., Barreto, S. M., Ostrosky, E. A., Da Rocho-Filho, P. A., Verissimo, L. M. and Ferrari, M. (2015). Production and characterisation of cosmetic nanoemulsions containing Opuntia ficusindica (L.) mill extract as moisturizing agent. Molecules, 20(2): 2492-2509.

- Hadzir, N. M., Basri M., Rahman, M. B. A., Salleh, A. B., Rahman, R. N. Z. R. A., and Basri H. (2013). Phase behaviour and formation of fatty acid esters nanoemulsions containing piroxicam. AAPS PharmSciTech, 4:456-63.

- Yılmaz, B., Kadıoğlu, Y. and Aksoy, Y. (2003). Simultaneous determination of gemcitabine and its metabolite in human plasma by high-performance liquid chromatography. Journal of Chromatography B, 791(1): 103-109.

- Xu, H., Paxton, J., Lim, J., Li, Y., and Wu, Z. (2014). Development of a gradient high-performance liquid chromatography assay for simultaneous analysis of hydrophilic gemcitabine and lipophilic curcumin using a central composite design and its application in liposome development. Journal of Pharmaceutical and Biomedical Analysis, 98: 371-378.

- Zidan, A. S., Kamal, N., Alayoubi, A., Seggel, M., Ibrahim, S., Cruz, C., and Ashraf, M. (2017). Effect of isopropyl myristate on transdermal permeation of testosterone from carbopol gel. Journal of Pharmaceutical Sciences, 106(7): 1805-1813.

- Oliveira, J. S. L., Lange, S., Dobner, B., and Brezesinski, G. (2017). The effect of non-deuterated and deuterated isopropyl myristate on the thermodynamical and structural behavior of a 2D stratum corneum model with ceramide. Chemistry and Physics of Lipids, 204: 1-9.

- Hwang, T. L, Fang, C. L, Chen, C. H, and Fang, J. Y. (2009). Permeation enhancer containing water-in-oil nanoemulsions as carriers for intravesical cisplatin delivery. Pharmaceutical Research, 26(10): 2314-2323.

- Prajapati, H. N., Dalrymple, D. M., Serajuddin, A. T. M., Agu, R. U., Ugwoke, M. I., Armand, M., and Mehta, S. K. (2016). Formulation and physiochemical study of a-tocopherol based oil in water nanoemulsion stabilised with non-toxic, biodegradable surfactant: Sodium stearoyl lactate. Ultrasonics Sonochemistry, 29(1): 285-305.

- Frasch-Melnik, S., Spyropoulos, F., and Norton, I. T. (2010). W1/O/W2 double emulsions stabilised by fat crystals: Formulation, stability and salt release. Journal of Colloid and Interface Science. 350(1): 178-185.

- Matos, M., Gutierres. G., Coca, and J., Pazos, C. (2014). Preparation of water-in-oil-water (W/O/W) double emulsions containing trans-resveratrol. Colloids and Surfaces A: Physicochemical and Engineering Aspects, (442):69-79.

- Park, C. I., Cho, W., and Lee, S. J. (2003). Emulsion stability of cosmetic creams based on water-in-oil high internal phase emulsions Emulsion stability of cosmetic creams based on water-in-oil high internal phase emulsions. Korea-Australia Rheology Journal, 15(3): 125-130.

- Paunivic, M. and Schlesinger, M. (2006). Fundamentals of deposition (second edition). New Jersey: John Wiley & Sons, Inc.

- Márquez, A. L., Medrano, A., Panizzolo, L. A. and Wagner, J. R. (2010). Effect of calcium salts and surfactant concentration on the stability of water-in-oil (w/o) emulsions prepared with polyglycerol polyricinoleate. Journal of Colloid and Interface Science, 341(1): 101-108.

- Wahgiman, N. A., Salim, N., Abdul Rahman, M. B. and Ashari, S. E. (2019). Optimization of nanoemulsion containing gemcitabine and evaluation of its cytotoxicity towards human fetal lung fibroblast (MRC5) and human lung carcinoma (A549) cells. International Journal of Nanomedicine, 14: 7323-7338.

- Sulaiman, I. S. C., Basri, M., Fard Masoumi, H. R., Ashari, S. E., Basri, H., and Ismail, M. (2017). Predicting the optimum compositions of a transdermal nanoemulsion system containing an extract of Clinacanthus nutans leaves (L.) for skin antiaging by artificial neural network model. Journal of Chemometrics, 31(7): 1-13.

- Shakeel, F., Haq, N., Al-dhfyan, A., Alanazi, F. K. and Alsarra, I. A. (2014). Double w/o/w nanoemulsion of 5- fluorouracil for self-nanoemulsifying drug delivery system. Journal of Molecular Liquids, 200: 183-190.

- Azhar, S. N. A. S., Ashari, S. E., and Salim, N. (2018). Development of a kojic monooleate-enriched oil-in-water nanoemulsion as a potential carrier for hyperpigmentation treatment. International Journal of Nanomedicine, 13: 6465-6479.

- Xavier-Júnior, F. H., Silva, K. G. H., Farias, I. E. G., Morais, A. R. V. and Alencar, E. N. (2012). Prospective study for the development of emulsion systems containing natural oil products. Journal Drug Delivery and Science Technology, 22(4): 367-372.

- Latreille, B., and Paquin, P. (1990). Evaluation of emulsion stability by centrifugation conductivity measurements. Journal of Food Science, 55(6): 1666-1669.

- Izadiyan, Z., Basri, M., Fard Masoumi, H. R., Abedi Karjiban, R., Salim, N. and Shameli, K. (2017). Modeling and optimization of nanoemulsion containing Sorafenib for cancer treatment by response surface methodology. Chemistry Central Journal, 11(1): 21.

- Ramli, S., Zainuddin, N., Mohamad, S., and Rahman, I. A. (2017). Nanoemulsion based palm olein as vitamin E carrier. Malaysian Journal of Analytical Sciences, 12(6): 1399-1408.