S

# EFFECT OF Cr2O3 ON THE TRANSITION TEMPERATURE AND PHASE FORMATION OF Tl2-xCrxBa2CaCu2O8-δ SUPERCONDUCTOR

# (Kesan Cr2O3 Terhadap Suhu Peralihan dan Pembentukan Fasa Superkonduktor 
Tl2-xCrxBa2CaCu2O8-δ)

Syahrul Humaidi1* and Roslan Abd-Shukor2

# 1Department of Physics,

# FMIPA-Universitas Sumatera Utara, Jln Bioteknologi 1, Medan 20155, Indonesia

# 2Department of Applied Physics,

# Universiti Kebangsaan Malaysia, 43600 UKM Bangi, Selangor, Malaysia

# *Corresponding author:  syahrul1@usu.ac.id

Received: 13 November 2019; Accepted: 3 September 2020; Published: xx October 2020

Abstract

The Tl-based high Tc superconductors, Tl2-xCrxBa2CaCu2O8-δ (Tl2212) have been prepared via the solid-state reaction method. The substitution of Cr into the Tl-site was aimed to investigate the role of Cr on the transition temperature and phase stability of the Tl2212 phase. Ba2CaCu2Oy precursor material was synthesized using BaCO3 (99.9%, Aldrich), CaO (99.99%, Alfa Aesar), and CuO (99.9%, Alfa Aesar) powder as the starting compound. The powders were mixed and sintered at 900 oC for 24 hours before cooled to room temperature. The precursor was mixed with Tl2O3 (99.9%, Alfa Aesar) and Cr2O3 (99.9%, Merck) powders before being pressed to obtain Tl2-xCrxBa2CaCu2O8 pellet. The pellets were heated at 900 oC with oxygen flow for 4 minutes. The transition temperature, Tc was determined using the standard four-point probe electrical resistance measurements from 50 K to 300 K with a constant current of 20 mA. The phases were determined by powder X-ray diffraction (XRD) method using CuKα source with λ= 1.5418 Å. Based on XRD analysis, the x = 0, 0.2, and 0.6 showed unit cell belonging to the 14/mmm space group. In the x = 0.4, the space group changed to P4/mmm which is the Tl1212 phase. It was found that the optimum composition was Tl1.8Cr0.2Ba2CaCu2O8-δ and the maximum zero-resistance temperature, Tc-zero was 96 K, and the onset temperature, Tc-onset was 116 K. It was observed that the transition temperatures decreased with increasing Cr2O3. The volume fraction of the Tl2212 phase in this composition was 88% with the c-lattice parameter equals to 29.388Å. Superconductivity was destroyed in the x = 1.0 samples.

Keywords:  transition temperature, structure, Tl2212 phase

# Abstrak

# Superkonduktor suhu tinggi berasaskan Tl iaitu, Tl2-xCrxBa2CaCu2O8-δ (Tl2212) telah disediakan melalui kaedah tindak balas pepejal. Penggantian Cr pada kedudukan Tl dilakukan untuk menyelidik peranan Cr terhadap suhu genting dan kestabilan fasa superkonduktor Tl2212. Bahan pelopor Ba2CaCu2Oy disintesis dengan menggunakan serbuk BaCO3(99.9%, Aldrich), CaO(99.99%, Alfa Aesar) dan CuO(99.9%, Alfa Aesar) sebagai campuran awal. Serbuk ini kemudiannya disinter pada 900 oC selama 24 jam dan dibiarkan sejuk sehingga suhu bilik. Bahan pelopor ini kemudianmya dicampurkan dengan serbuk Tl2O3 (99.9%, Alfa Aesar) dan serbuk Cr2O3(99.9%, Merck) untuk menghasilkan pelet Tl2-xCrxBa2CaCu2O8. Pelet kemudiannya disinter pada 900 oC dengan aliran gas oksigen selama 4 minit. Suhu peralihan, Tc ditentukan dengan pengukuran rintangan elektrik menggunakan kaedah piawai empat titik dalam suhu 50 K hingga 300K dengan bekalan arus malar 20 mA. Pecahan fasa diperolehi daripada kaedah pembelauan serbuk sinar-X (XRD) menggunakan sinar CuKα dengan panjang gelombang λ= 1.5418Å. Berdasarkan analisis XRD, sampel x = 0, 0,2, dan 0.6 adalah pada kumpulan ruang 14/mmm. Untuk sampel x = 0.4 kumpulan ruang berubah menjadi P4/mmm iaitu fasa yang berlainan (Tl1212). Didapati bahawa suhu peralihan sifar maksimum, Tc sifar adalah 96 K dan suhu perlalihan mula, Tc mula adalah 116 K bagi komposisi Tl1.8Cr0.2Ba2CaCu2O8-δ. Pecahan isipadu daripada fasa Tl2212 dalam sampel ini adalah 88% dengan parameter kekisi c bersamaan 29.388 Å. Sifat superkonduktor hilang pada komposisi x = 1.0.

# Kata kunci:  suhu peralihan, struktur, fasa Tl2212

Introduction

High temperature superconductor (HTSC) based on copper oxides have critical temperature greater than 77 K (above liquid nitrogen temperature). Some of the common types of HTSCs include YBaCuO (YBCO), BiSrCaCuO (BSSCO), TlBaCaCuO (TBCCO), HgBaCaCuO, and HgTlBaCaCuO.  Many efforts are being made to enhance the transition temperature of HTSCs. Some researchers modified the fabrication techniques of the materials [1-4]. Most of the research works [5-9] deal with doping and atomic substitution. The thallium-based copper oxide superconductor consists of several phases with a different number of copper oxide layers.  Previous works on thallium-based high temperature superconductor concentrated on several phases of Tl-based HTSCs.  Tc of TlBa2CaCu2O7-δ (Tl1201) was around 70 K [10], whereas Tl2Ba2CaCu2O8-δ (Tl1212) had Tc of 110 K [11].  The TlBa2Ca3Cu4O11-δ (Tl1234) was reported with Tc of around 114 K [12].

The role of Cr at the Tl-sites in Tl-based superconductor has been widely studied. Chromium is an effective element for substitution in Tl-Sr-Ca-Cu-O systems [13]. There have been several reports on the effect of Cr on the superconductivity of Tl-1212 phase. The substitution of Cr for Tl or Ca site improves the superconducting behavior [11, 14, 15]. Cr substitution improves the critical temperature up to 110 K [16]. The Tl2Ba2CaCu2O8-δ samples with high purity were reported to have Tc of 106 K [17, 18]. The samples were prepared from metal oxides with a starting composition Tl2212 and heated at 900 oC for 24 hours followed by adding appropriate amounts of Tl2O3 and heated again at 915-920 oC for 4-5 minutes. In a previous report, it has been observed that the volume fraction of Tl2212 phase increased as Te content was increased [19]. It is interesting to investigate the effects of Cr in other phases of the Tl-based superconductor.  In this paper, we report the effects of Cr on the superconducting properties and phase formation of the Tl-2212 phase.

# Materials and Methods

# Samples with the nominal starting composition (Tl2-xCrx)Ba2CaCu2O8 with x = 0.0, 0.2, 0.4, 0.6, and 0.8 were prepared by the solid state reaction method. Appropriate amounts of high purity (>99.99%) BaCO3, CaO, and CuO were mixed completely using an agate mortar to obtain a homogeneous mixture. The precursor powders were heated at 900 °C for 24 hours with several intermittent grinding. Appropriate amounts of Tl2O3 and Cr2O3 with appropriate mole% were then added to the precursor and completely mixed before being pressed into pellets with 1.3 cm diameter and 0.2 cm thickness under 7 ton/cm2 of pressure.  The pellets were heated at 900 °C in flowing oxygen for 4 minutes.  This was followed by furnace cooling to room temperature. An excess of 10% Tl2O3 was added to compensate for the thallium lost during heating.

# The dc electrical resistance measurements were performed between 50 K and 300 K.  The four-point method with silver paste contact was used for the measurement.  A closed cycle refrigerator from CTI Cryogenic Model 22 cryostat and a temperature controller from Lake Shore Temperature Controller Model 340 was employed. A constant current source between 1 mA and 100 mA was used throughout the measurements. The powder X-ray diffraction (XRD) method was used to identify the phases. A Bruker model D8 Advance diffractometer with CuKα radiation source with λ=1.5418Å was used. A software from Eva program was used to analyze the XRD patterns.

Results and Discussion

The curves of electrical resistance as a temperature function are shown in Figures 1(a) to 1(d).  Samples with x = 0.0- 0.6 showed metal-like behaviour above the transition temperature. For x = 0 the resistance dropped abruptly at 105 K, where it is defined as Tc onset. The zero resistance occurs at 93 K and is denoted as Tc-zero.  A narrow transition width ΔTc of 12 K was observed. For samples with x = 0.2, Tc-onset was observed to increase to 116 K and Tc-zero was 96 K. However, ΔTc increased to 20 K. When the content of Cr was increased to x = 0.4, Tc-onset decreased to 105 K. A drastic decrease of Tc-onset occurred for x = 0.6 with Tc-onset of 84 K and a narrower ΔTc of 13 K. Samples with x = 0.8 showed a high Tc-onset, but Tc-zero decreased to 60 K. This is due to the high resistivity in the normal state (Table 1). It is interesting to note that superconductivity was not observed in the x = 1.0 sample. The transition temperatures and room temperature resistivity of Tl2-xCrxBa2CaCu2O8-δ is presented in Table 1.

A previous finding on the Tl-1212 phase using Cr2S3 as a source of Cr [18] reported that Tc-onset is between 90 K and 105 K. This is due to the high resistivity in the normal state. In this work the highest Tc-onset as well as Tc-zero was observed in the x = 0.2 samples indicating an optimal doping level was achieved. This also coincided with the lowest normal state resistivity at 297 K, which indicates the optimization of hole concentration as a result of Cr substitution [20]. Using XRD patterns and analysis by EVA programme, the lattice parameters were calculated and presented in Table 2.

# Table 2 shows the phases in the samples which consist of the Tl1212, Tl2223, Tl1223, Tl2234, and Tl1234 phases. It is noted that the Tl2212 phase was present with a volume fraction between 50% and 88%. The occurrence of multi phases in the x = 0.8 sample resulted in the reduction of Tc-zero to 60 K. The samples were in 14/mmm and P4/mmm space group for x = 0.0 and x = 0.6. In the x = 1.0 samples, superconductivity was completely suppressed and the sample became insulating.  This was due to the presence of unknown phases.

- (b)

(c) (d)

Figure 1.   Electrical resistance as a function of temperature for Tl2-xCrxBa2CaCu2O8-δ with (a) x = 0, (b) x = 0.2, (c)

x 0.4 and  (d) x = 0.6

Table 1.  Transition temperatures and electrical resistivity at 297 K of Tl2-xCrxBa2CaCu2O8-δ

| x | Tc-zero ( + 1 K) | Tc-onset (+1 K) | ΔTc (+ 1 K) | ρ 297 K(Ωcm) |
| --- | --- | --- | --- | --- |
| 0 | 93 | 105 | 12 | 0.1562 |
| 0.2 | 96 | 116 | 20 | 0.1249 |
| 0.4 | 84 | 105 | 21 | 0.5966 |
| 0.6 | 71 | 84 | 13 | 0.5220 |
| 0.8 | 60 | 104 | 64 | 0.6072 |
| 1.0 | - | - | - | - |

Table 2.  Phases occurrence, volume fraction, and space group of the samples

| Sample | Tl-2212 Phase (%) | Tl-1212 Phase (%) | Tl-1223 Phase (%) | Tl-2223 Phase (%) | Tl-2201 Phase (%) | Tl-2234 Phase (%) | Other Phase (%) | Space group |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| x = 0.0 | 50 | 8 | 0 | 0 | 27 | 0 | 0 | 14/mmm (139) |
| x = 0.2 | 83 | 6 | 0 | 6 | 0 | 6 | 0 | 14/mmm (139) |
| x = 0.4 | 88 | 6 | 0 | 0 |  | 6 | 0 | P4/mmm |
| x = 0.6 | 68 | 4 | 4 | 12 | 0 | 4 | Tl-1234 (4) | 14/mmm (139) |
| x = 0.8 | 46 | 4 | 4 | 4 | 0 | 15 | Tl-1234 (15) | Pnma (60) |
| x = 1.0 | 40 | 0 | 0 | 20 | 6 | 8 | Tl-1234 (2) Unknown/22 | - |

Conclusion

We have prepared Tl2212 superconductor via the solid-state reaction method. The addition of Cr into (Tl2-xCrx)Ba2CaCu2O8) has significantly affected the transition temperature. The volume fraction of the Tl2212 phase should be considered in the enhancement of transition temperature. Based on our experiments, it was found that the Tl1.8Cr0.2Ba2CaCu2O8-δ sample can be used as a starting composition for further investigation.

# Acknowledgement

This research was supported by the Ministry of Higher Education of Malaysia under grant no. FRGS/1/2017/STG02/UKM/01/1.

References

- Ahmad, K. Y. and Abd-Shukor, R. (2003). Synthesis and formation of Tl-1223 and Tl-2223 high-Tc superconductors. Pertanika Journal Science & Technology, 11(1): 1-7.

- Ji, L., Yan, S. L., Zhao, X. J., Fang, L., Li, Y. G., He, M., Zhou, T. G., Chai, C., Eickmeye, J. and Holzapfel, B. (2006). Preparation and characterization of Tl2Ba2CaCu2O8. Superconductor Science Technology, 19: 338-341.

- Cheng, Z. X., Wang, X. L., Keshavarzi, S., Qin, M. J., Silver, T. M., Liu, H. K., Kimura, H. and Dou, S. X. (2004). The morphology, periodical modulation structure and effects of heat treatment on the superconductivity of (Tl,Pb)(Sr,Ba)-1223 single crystal. Superconductor Science Technology, 17: 696-700.

- Dark, C. J., Speller, S. C. and Grovenor, C. R. M. (2006). The development of bi-epitaxial texture and high grain boundary Jc values in Tl-2212 films on MgO substrate. Superconductor Science Technology, 19: 484-492.

- Pu, M. H., Cao, Z. S., Wang, Q. Y. and Zhao, Y.  (2006). The influence of Cr-ions on the flux creep in Bi-2223/Ag tapes. Superconductor Science Technology, 19: 462-465.

- Kong, W. and Abd-Shukor, R. (2007). Effect of nano Cr2O3 addition on (Bi,Pb)-Sr-Ca-Cu-O superconductor. Solid State Science and Technology, 15(1): 1-5.

- Ihara, H. and Sekita, Y.  (2001). United States Patent, US006300284B1 (10) Patent No:(45) Patent:US 6,300,284 B1.

- Jorda, J. L., Hopfinger, Th., Couach, M., Pugnat, P., Bertrand, C and Galezl, Ph. (1998). Formation of thallium-1223 superconductors. Journal of Superconductivity, 11(1): 87-89.

- Faizah, M. S., Yahya, A. K., Hamadneh, I. and Abd-Shukor, R. (2002). Effects of Ag addition and properties of Tl-2212 superconductors. Solid State Science and Technology, 10(1 & 2): 30-36.

- Kikuchi, M., Ohshima, E., Ohninshi, N., Muraoka, Y.,  Nakajima, S., Aoyagi, E., Ogawa, M., Akimitsu, J., Oku, T., Hiraga, K. and Syono, Y. (1994) Synthesis and superconductivity of oxycarbonates of the Tl-1201 phase. Physica C, 219(1-2):200-204.

- Abd-Shukor, R., Baharuddin, Y. and Lau, R. S. L. (1997). Formation of Tl-1212 phase in (Tl0.8M0.2)Sr2(Ca,Cr)Cu2O7  (M:Cd, and Sc) High-Tc superconductor, Journal of Materials Science Letters, 16: 818-820.

- Ogborne, D. M. and Weller, M. T. (1994). Oxygen non-stoichiometry in the (Tl,Pb)-Sr-Ca-Cu-O 1212 system. Physica C, 220: 389-395.

- Ranjbar, M. G. and Abd-Shukor, R. (2016). Excess conductivity and superconducting fluctuation analysis of Cr-substituted Tl-1223 type phase Tl1−xCrx)Ba2Ca2Cu3O9−δ (x = 0.4–0.8). Journal of Superconductor and Novel Magnetism, 29: 2235-2240.

- Abd-Shukor, R. and Quah, C. T. (1994) Superconductivity of 1212-type phase TlSr2(Ca,Cr)Cu2O7 and TlSr2(Sr,Tm)Cu2O7. Journal of Materials Science and Engineering B, 23: 54-57.

- Li, Y. F., Chmaissem, O., and Sheng, Z. Z. (1995). Crystal structure and Tc of 1212-type cuprate (Tl,Cr)Sr2(Ca,Tl) Cu2O7. Physica C, 248: 42-48.

- Sheng, Z. Z., Gu, D. X., Xin, Y. and Pederson. (1991). A new 1212-type phase Cr-substituted TlSr2CaCu2O7 with Tc up to about 110K. Modern Physics Letters B, 9:635-642.

- Abd-Shukor, R.(2002). The ubiquitous superconductor: Materials and mechanism. Solid State Science and Technology, 10(1&2): 14-21.

- Al-Sharabi, A., and Abd-Shukor, R. (2013) Formation of (Tl1-x Crx) Sr2CaCu2O7-δ (Tl-1212) Superconducting Phase Using Cr2S3. International Journal Electrochemical Sciences, 8: 7825-7830.

- Humaidi, S., Marlianto, E., Marhaposan, S. and Abd-Shukor, R. (2019). Superconducting properties of Te-substituted (Tl2-xTex)Ba2CaCu2O8-δ. Solid State Phenomena, 290: 239-244.

- Yusuf, A. A., Yahya, A. K., Khan, N. A., Salleh, F. M. D., Marsom, E and Huda, N. (2011). Effect of Ge4+ and Mg2+ doping on superconductivity, fluctuation induced conductivity and interplanar coupling of TlSr2CaCu2O7-δ superconductors. Physica C, 471:363-372.