Malaysian Journal of Analytical Sciences Vol 24 No 5 (2020): 757 - 765

# EQUIVALENT CIRCUIT ANALYSIS OF LaZrTa3O11 CERAMIC SYNTHESISED BY USING THE CONVENTIONAL SOLID-STATE METHOD

# (Analisis Litar Sepadan Seramik LaZrTa3O11 Disintesis dengan Menggunakan Kaedah Keadaan Pepejal Konvensional)

# Fadhlina Che Ros* and Jumiah Hassan

# Physics Department, Centre for Defence Foundation Studies,

# Universiti Pertahanan Nasional Malaysia, Kem Sungai Besi 57000, Kuala Lumpur, Malaysia

# *Corresponding author:  fadhlina@upnm.edu.my

Received: 13 November 2019; Accepted: 3 September 2020; Published:  xx October 2020

Abstract

# LaZrTa3O11 ceramic with α-U3O8-type structure has been prepared by using the conventional solid state-route and studied by using powder X-ray diffraction for phase analysis and impedance spectroscopy for electrical measurements. It has hexagonal unit cell with space group P6322 at room temperature. LaZrTa3O11 is reported to be isostructural with CaTa4O11 and Ag2Nb4O11; the structure is related to U3O8-structure, where it consists of single layers of edge-sharing pentagonal Ta-O bipyramids alternating with layers of edge-sharing octahedra. The impedance spectroscopy response showed that LaZrTa3O11 exhibited a typical insulating behaviour at room temperature, with permittivity, ε ~ 19. It was a highly resistive material with R >> 109 Ω at temperature below 500o C and as the temperature increased, frequency-dependence of alternating current conductivities at high frequency was clearly visible. The electrical properties of LaZrTa3O11 is best modelled by using non-Debye response circuit that consists of a parallel combination of a resistor, capacitor, and a constant phase element.

# Keywords:  LaZrTa3O11, dielectrics, high-temperature ceramics, lanthanide-oxide, non-Debye circuit

# Abstrak

# Seramik LaZrTa3O11 dengan struktur jenis α-U3O8 telah disediakan melalui kaedah keadaan pepejal konvensional dan dikaji dengan menggunakan pembelauan sinar-X untuk analisis fasa dan spektroskopi impedans untuk kajian sifat keelektrikan. Ia mempunyai sel unit heksagonal dengan kumpulan ruang P6322 pada suhu bilik. LaZrTa3O11 dilaporkan mempunyai sama struktur dengan CaTa4O11 dan Ag2Nb4O11; struktur tersebut adalah berkait dengan struktur U3O8 di mana ia terdiri daripada satu lapisan pentagonal bypiramid Ta-O berkongsi-sisi, berselang-seli dengan lapisan-lapisan oktahedra yang berkongsi-sisi. Tindak-balas spektroskopi impedans menunjukkan bahawa seramik LaZrTa3O11 mempamerkan sifat penebat yang tipikal pada suhu bilik, dengan kebolehtelapan, ε ~ 19. Ia adalah bahan berkerintangan tinggi dengan R >> 109 Ω pada suhu di bawah 500o C dan apabila suhu meningkat, kebergantungan frekuensi konduktiviti arus ulang alik pada frekuensi tinggi jelas kelihatan. Model terbaik sifat keelektrikan bagi seramik LaZrTa3O11 adalah menggunakan litar non-Debye yang terdiri daripada kombinasi selari perintang, kapasitor dan elemen fasa pemalar.

# Kata kunci:  LaZrTa3O11, dielektrik, seramik bersuhu tinggi, oksida lanthanid, litar non-Debye

References

- Masó, N., Woodward, D. I., Thomas, P. A., Várez, A. and West, A. R. (2011). Structural characterisation of ferroelectric Ag2Nb4O11 and dielectric Ag2Ta4O11. Journal of Materials Chemistry, 21: 2715-2722.

- Grins, J. and Nygren, M. (1992). Structure of LaZrTa3O11, a CaTa4O11 isotype. Materials Research Bulletin, 27: 141-145.

- Masó, N., Woodward, D. I., Thomas, P. A., Várez, A. and West, A. R. (2011). Polymorphism, structural characterisation and electrical properties of Na2Nb4O11. Journal of Materials Chemistry, 21: 12096-12102.

- Fadhlina Che Ros, Mclaren, N. R., Masó, N. and West, A. R. (2018). Synthesis, structure and dielectric properties of a new family of phases, ABC3O11: A = La, Pr, Nd, Sm, Gd; B = Zr, Hf; C = Ta, Nb. Journal of Australian Ceramic Society, 54: 1-10.

- Jahnberg, L. (1970). Crystal structures of Na2Nb4O11 and CaTa4O11. Journal of Solid State Chemistry, 1: 454-462.

- Zheng, C. and West, A. R. (1991). Compound and solid-solution formation, phase equilibria and electrical properties in the ceramic system ZrO2-La2O3-Ta2O5. Journal of Materials Chemistry, 1(2): 163-167.

- Moulson, A. J. and Herbert, J. M. (2008) Electroceramics. John Wiley & Sons: pp. 285.

- Joncher, A. K. (1983). Dielectric relaxation in solids. chelsea dielectric press. London: pp. 209.

- Scarel, G., Svane, A. and Fanciulli, M., (2007). Scientific and technological issue related to rare–earth oxides: An introduction.  Journal of Applied Physics, 106: 1-14.