Malaysian Journal of Analytical Sciences Vol 25 No 2 (2021): 296 - 310

# SENSOR ION Al3+ OPTIK BERASASKAN ERIOKROM SIANIN R TERPEGUN DALAM MEMBRAN POLIMER TERANGKUM MENGGUNAKAN PRINSIP PENGUKURAN SERAPAN

# (An Optical Sensor For Al3+ Ion Based on Immobilized Eriochrome Cyanine R

# in Polymer Inclusion Membrane using Absorption Sensing Principle)

# Faiz Bukhari Mohd Suah1*, Musa Ahmad2, Lee Yook Heng3

# 1Green Analytical Chemistry Laboratory, School of Chemical Sciences,

# Universiti Sains Malaysia, 11800 Minden, Pulau Pinang, Malaysia

# 2Faculty of Science and Technology,

# Universiti Sains Islam Malaysia, 71800 Nilai, Negeri Sembilan, Malaysia

# 3School of Chemical Sciences and Food Technology, Faculty of Science and Technology,

# Universiti Kebangsaan Malaysia, 43600 UKM Bangi, Selangor, Malaysia

# *Pengarang Utama:  fsuah@usm.my

Received: 7 February 2021 ; Accepted: 18 March 2021; Published:  25 April 2021

Abstrak

# Sensor optik bagi pengesanan ion aluminium (Al3+) berasaskan reagen terpegun dalam membran polimer terangkum (PIM) telah dibangunkan dalam kajian ini. Sensor ini menggunakan eriokrom sianin R (ESR) sebagai reagen dan prinsip pengukuran serapan sebagai kaedah pengesanan ion Al3+. Bahan sensor PIM yang digunakan dalam kajian ini mengandungi selulosa triasetat 60% berat (m/m): Aliquat 336 30% berat (m/m): dioktil ftalat 10% berat (m/m) dan ESR dengan kepekatan 5.00 × 10-4 mol L-1. Sensor berasaskan PIM ini menghasilkan rangsangan yang lebih tinggi berbanding sensor tidak berasaskan PIM. Masa optimum rangsangan sensor ialah pada lima minit dengan nilai pH optimum 6.0. Sensor ini memberikan julat rangsangan linear pada julat kepekatan ion Al3+ 7.41 × 10-6 - 4.44 × 10-4 mol L-1, dengan had pengesanan terendah 5.63 × 10-6 mol L-1. Sifat kepilihan yang tinggi kepada ion Al3+ turut ditunjukkan oleh sensor ini kecuali gangguan minima daripada ion Be2+ dan Fe3+. Akhir sekali, sensor ini telah digunakan bagi penentuan ion Al3+ dalam beberapa sampel air semula jadi. Keputusan analisis menunjukkan sensor ini mampu menghasilkan keputusan yang setara dengan spektrofotometer serapan atom konvensional.

# Kata kunci:  sensor Al3+, Aliquat 336, eriokrom sianin R, membran polimer terangkum

# Abstract

# An optical sensor for aluminium ion (Al3+) based on immobilized reagent in polymer inclusion membrane (PIM) was developed in this study. This sensor utilized eriochrome cyanine R (ECR) as its reagent and absorption sensing principle as the method for Al3+ ion sensing. PIM’s sensing material used in this study consists of cellulose triacetate 60% mass (m/m): Aliquat 336 30% mass (m/m): dioctyl phthalate 10% mass (m/m) and ECR with concentration of 5.00 × 10-4 mol L-1. This sensor which based on immobilized PIM produced higher response compared to sensor based on non-immobilized PIM. Optimum response time of this sensor was five minutes with an optimum pH value of 6.0. This sensor also produced a linear response range for Al3+ ion concentration of 7.41 × 10-6 - 4.44 × 10-4 mol L-1, with detection limit of 5.63 × 10-6 mol L-1. High selectivity towards Al3+ ion was also demonstrated by this sensor, except minimal interferences from Be2+ and Fe3+ ions. Finally, this sensor was applied for the determination of Al3+ ion in natural water samples. Results shows this sensor is capable of producing comparable output to conventional atomic absorption spectrophotometer.

Keywords:  Al3+ sensor, Aliquat 336, eriochrome cyanine R, polymer inclusion membrane

# Rujukan

- Shetty, R., Vidya, C. S. N., Prakash, N. B, Lux, A. and Vaculik, M. (2021). Aluminium toxicity in plants and its possible mitigation in acid soils by biochar: A review. Science of the Total Environment, 765: 142-744.

- Yokel, R. A. (2020). Aluminum reproductive toxicity: a summary and interpretation of scientific reports. Critical Reviews in Toxicology, 50: 551-593.

- Dórea, J. G. (2020). Neurotoxic effects of combined exposures to aluminum and mercury in early life (infancy). Environmental Research, 188: 109734.

- Gürses, A., Açıkyıldız, M., Güneş, K. and Gürses, M. S. (2016). Dyes and pigments. Springer, Berlin: pp 13-29.

- Mohd Suah, F. B., Ahmad, M. and Lee, Y. H. (2016). Kesan penambahan surfaktan tak-ionik kepada kompleks Al(III)-ESR dalam penentuan aluminium(III) akues secara spektrofotometri. Sains Malaysiana, 45: 1807-1814.

- Nizar, S. A., Satar, N. S. A., Amar, S. A. S., Abdullah, F. H., Mehamod, F. S., Suah, F. B. M. (2019). Fluorescence enhancement of Al3+ - sodium morin-5-sulfonate complex by imidazolium ionic liquid and its application in determination of Al3+ ions in an aqueous solution. Jurnal Teknologi, 81: 175-180.

- Mohd Suah, F. B., Ahmad, M. and Lee, Y. H. (2014). Highly sensitive fluorescence optode based on polymer inclusion membranes for determination of Al(III) ions. Journal of Fluorescence, 24: 1235-1243.

- Chebotaryov, A. N., Snigur, D.V., Duboviy, V. P., Scherbakova, T. M., Bevziuk, K. V. and Nevmerjitcaia, K. S. (2017). The features of pyrocatechol violet complexation with Mo(VI) and W(VI) in solutions. The spectrophotometric determination of Mo(VI) in multivitamins. Methods and Objects of Chemical Analysis, 12: 12-16.

- Wang, X. D. and Wolfbeis, O. S. (2020). Fiber-optic chemical sensors and biosensors (2015-2019). Analytical Chemistry, 92: 397-430.

- Makowka, A. and Pospiech, B. (2019). Synthesis of polymer inclusion membranes based on cellulose triacetate for recovery of lanthanum(III) from aqueous solutions. Autex Research Journal, 19: 288-292.

- Ncib, S., Barhoumi, A., Bouguerra, W., Larchet, C., Dammak, L., Hamrouni, B. and Elaloui, E. (2018). Preparation and characterization of cellulose triacetate polymer inclusion membrane blended with acetylated kraft lignin: Effect of akl and application to the copper(II) extraction from acidic media. Desalination and Water Treatment, 104: 263-272.

- Radzyminska-Lenarcik, E., Pyszka, I. and Ulewicz, M. (2020). Separation of Zn(II), Cr(III), and Ni(II) ions using the polymer inclusion membranes containing acetylacetone derivative as the carrier. Membranes, 10: 88.

- Mohd Suah, F. B. and Ahmad. M. (2017). Preparation and characterization of polymer inclusion membrane based optode for determination of Al3+ ion. Analytica Chimica Acta, 951: 133-139.

- Abdullah, F. H., Latif, N. A. A., Suah, F.B.M. and Mehamod, F.S. (2017). Sensitive fluorimetric determination of Al3+ ion based on the formation of ternary complex containing room temperature ionic liquid. Journal of Luminescence, 188: 267-274.

- Du, X. and Xie, X. (2021). Ion-selective optodes: alternative approaches for simplified fabrication and signaling. Sensors Actuators B: Chemical, 335: 129368.

- Mohd Suah, F. B. (2017). Preparation and characterization of a novel Co(II) optode based on polymer inclusion membrane. Analytical Chemistry Research, 12: 40-46.

- Denna, M. C. F. J., Camitan, R. A. B., Yabut, D. A. O., Rivera, B. A. and Coo, L. D. (2018). Determination of Cu(II) in environmental water samples using polymer inclusion membrane-TAC optode in a continuous flow system. Sensors Actuators B: Chemical, 260: 445-451.

- Khajehsharifi, H., Bordbar, M. M. and Esfandiary, P. (2018). Design and evaluation of a novel bismuth optical sensor using PC-ANN application. Analytical and Bioanalytical Chemistry Research, 5: 159-169.

- Miller, J. N., and Miller, J. C. (2018). Statistics and chemometrics for analytical chemistry. 7th Edition. Pearson/Prentice Hall, Harlow: pp 1-30.

- Mohd Suah, F. B., Mehamod, F. S. and Ahmad, M. (2017). Effect of non-ionic surfactants to the Al(III)-morin complex and its application in determination of Al(III) ions: a preliminary study. Malaysian Journal of Analytical Sciences, 21: 793–800.

- Ramadan, M. S., El-Mallah, N. M., Nabil, G. M. and Abd-Elmenem, S. M. (2019). Hydrophobic effect for anionic dye - cationic surfactant interaction in aqueous and mixed solvent. Journal of Dispersion Science and Technology, 40: 1110–1120.

- Anwar, Z. M., Ibrahim, I. A., Kamel, R. M., Abdel-Salam, E. T. and El-Asfoury, M. H. (2018). New highly sensitive and selective fluorescent terbium complex for the detection of aluminium ions. Journal of Molecular Structure, 1154: 272-279.

- Yıldız, E., Saçmacı, Ş., Saçmacı, M. and Ülgen, A. (2017). Synthesis, characterization and application of a new fluorescence reagent for the determination of aluminum in food samples. Food Chemistry, 237: 942-947.

- Nguyen, M. P., Kelly, S. P., Wydallis, J. B. and Henry, C. S. (2020). Read-by-eye quantification of aluminum (III) in distance-based microfluidic paper-based analytical devices. Analytica Chimica Acta, 1100: 156-162.

- Harris, D. C. and Lucy, C. A. (2020). Quantitative chemical analysis. 10th Edition. Freeman WH, New York: pp 99-126.