Malaysian Journal of Analytical Sciences Vol 25 No 4 (2021): 642 - 648

COLOUR STRENGTH AND WASH FASTNESS OF SILK FABRIC DYED WITH METHANOLIC EXTRACTED RANGOON CREEPER USING INFRA-RED DYEING MACHINE

(Kekuatan Warna dan Ketahanan Cucian Kain Sutera Diwarnakan dengan Akar Dani yang Diekstrak dengan Pelarut Metanol Menggunakan Mesin Pencelup Infra-Merah)

Suhaidi Ariffin1, Wan Syazehan Ruznan1*, Muhammad Nurkhairunizam Yazid2, Suraya Ahmad Suhaimi1,

Mu’adz Ahmad Mazian2, Muhammad Mu’az Mustamam2

1Clothing Innovation and Textile Research Association (CITRA),

2Faculty of Applied Sciences,

Universiti Teknologi MARA Cawangan Negeri Sembilan, Kampus Kuala Pilah, 72000 Kuala Pilah, Negeri Sembilan, Malaysia

*Corresponding author:  syazehan@uitm.edu.my

Received:  21 June 2021; Accepted: 11 August 2021; Published:  29 August 2021

Abstract

Extracting dyes from plant sources is one of the eco-friendly ways to reduce environmental pollution. Since the discovery of synthetic dyes back in 1856, the use of natural dyes in the textile industry has become lessen. This work focuses on the determination of new colours from Rangoon creeper petals through the methanolic extraction method and dyed by using an Infra-Red dyeing machine to generate a new colour pallet that is similar to PANTONE® colour and to study its wash fastness properties. Silk fabric was used and dyeing was carried out with calamansi and vinegar as the mordanting agents. Dyed silk samples were measured by using X-rite RM2000 Capsure to get the commercial PANTONE® colour code. The CIELAB colours coordinates were retrieved from the PANTONE® website and the L*a*b* values plotted indicates that all dyed silks were in the yellow-red quadrant. Colourfastness to washing shows an excellent rating i.e., 4/5, indicating outstanding stability. Thus, it was found that the colour produced from Rangoon creeper petals is suitable as a natural dye and also established high commercial value because the colour obtained is commensurate with the colour displayed by PANTONE® colours.

Keywords:  rangoon creeper, natural dye, methanol extraction, infra-red dyeing

Abstrak

Mengekstrak pewarna daripada tumbuhan adalah salah satu kaedah mesra alam untuk mengurangkan pencemaran alam sekitar. Sejak penemuan pewarna sintetik pada tahun 1856, penggunaan pewarna semula jadi dalam industri tekstil semakin berkurangan. Kajian ini memfokuskan kepada penemuan warna baharu daripada kelopak bunga akar dani melalui kaedah pengekstrakan metanol dan diwarnakan dengan menggunakan mesin pencelup Infra-Merah bagi menghasilkan palet warna baharu yang serupa dengan warna PANTONE®, serta mengkaji sifat ketahanan warna. Kain sutera digunakan dan pencelupan dilakukan dengan limau kasturi dan cuka sebagai agen pengikat. Sampel sutera yang dicelup diukur dengan menggunakan X-rite RM2000 Capsure untuk mendapatkan kod warna PANTONE® yang komersial. Koordinat warna CIELAB diambil dari laman web PANTONE dan nilai L*a*b* yang ditunjukkan menunjukkan bahawa semua sutera yang dicelup berada di kuadran kuning-merah. Ketahanan warna terhadap cucian menunjukkan tahap cemerlang iaitu 4/5. Oleh itu, didapati bahawa warna yang dihasilkan daripada kelopak akar dani sesuai sebagai pewarna semula jadi dan juga memiliki nilai komersial yang tinggi kerana warna yang diperolehi setara dengan warna yang ditunjukkan oleh warna PANTONE®.

Kata kunci:  akar dani, pewarna semulajadi, pelarut metanol, pencelupan infra-merah

References

- Kishor, R., Purchase, D. Saratale, G. D., Saratale, R. G., Ferreira, L. F. R., Bilal, M., Chandra, R. and Bharagava, R. N. (2020). Ecotoxicological and health concerns of persistent coloring pollutants of textile industry wastewater and treatment approaches for environmental safety. Journal of Environmental Chemical Engineering, 9(2): 1-18.

- Hassaan, A., M. (2017). Health and environmental impact of dyes: Mini review. American Journal of Environmental Science and Engineering 1(3): 64-67.

- Behera, M., Nayak, J., Banarjee, S., Chakrabortty, S. and Tripathy, S. K. (2021). A review on the treatment of textile industry waste effluents towards the development of efficient mitigation strategy: An integrated system design approach. Journal of Environmental Chemical Engineering 9(4): 1-21.

- Tkacyzk, A., Mitrowska, K. and Posyniak, A. (2020). Synthetic organic dyes as contaminants of the aquatic environment and their applications for ecosystems: A review. Science of the Total Environment 717: 1-19.

- Ludin, N. A., Al-Alwani, M.A.M., Mohamad, A. B., Kadhum, A. A. H., Hamid, N. H., Ibrahim, M. A., Teridi, M. A. M., Al-Hakeem, A., Mukhlus, A. and Sopian, K. (2018). Utilization of natural dyes from Zingiber officinale leaves and Clitoria ternatea flowers to prepare new photosensitiser for dye-sensitised solar cells. International Journal of Electrochemical Science, 13(2018): 7451-7465.

- Kim, H. J., Bin, Y.T., Karthick, S. N., Hemalatha, K. V., Raj, C. J., Venkatesan, S., Park, S. and Vijaykumar, G. (2013). Natural dye extracted from rhododendron species flowers as a photosensitizer in dye-sensitized solar cell. International Journal of Electrochemistry Science, 8: 6734-6743.

- Singh, S., Bothara, S. B. and Singh, S. (2011). Acid-base indicator properties of dye from local flowers: Cassia anugostifolia Linn., Thevetia peruviana (Pers.) K. Schum and Thevetia thvetiodes (Kunth) K. Schum. Pharmacognosy Journal, 3(19): 35-39.

- Sahu, J., Patel, P. K. and Dubey, B. (2012). Quisqualis indica Linn: A review of its medicinal properties. International Journal of Pharmaceutical and Phytopharmacological Research, 1(5): 313-321.

- Voon, Ching, H., Bhat, R. and Rusul, G. (2012). Flower extracts and their essential oils as potential antimicrobial agents for food uses and pharmaceutical applications. Comprehensive Reviews in Food Science and Food Safety, 11(1): 34-55.

- Soniya, M. and Anitha, D. (2018). Microwave extraction of dye from Madhumalti flower. Journal of Research Angrau, 46(4): 61-66.