Malaysian Journal of Analytical Sciences Vol 25 No 5 (2021): 882 - 894

# APPLICATION OF ZINC OXIDE NANOPARTICLES AND NANOCHITOSAN TO ENHANCE THE LIGHT FASTNESS OF COTTON DYED WITH NATURAL INDIGO

# (Aplikasi Zink Oksida Nanopartikel dan Nano Kitosan untuk Meningkatkan Ketahanan Pudar Kain yang Diwarnai Indigo Asli)

# Renung Reningtyas1,2, Edia Rahayuningsih1,3*, Yuni Kusumastuti1, Indriana Kartini3,4

# 1Department of Chemical Engineering, Faculty of Engineering,

# Universitas Gadjah Mada, 55281 Yogyakarta, Indonesia

# 2 Department of Chemical Engineering, Faculty of Industrial Engineering,

# Universitas Pembangunan Nasional “Veteran” Yogyakarta, 55283 Yogyakarta, Indonesia

# 3Indonesia Natural Dye Institute, Integrated Research and Testing Laboratory,

# 4Department of Chemistry, Faculty of Mathematics and Natural Sciences,

# Universitas Gadjah Mada, 55281 Yogyakarta, Indonesia

# *Corresponding author:  edia_rahayu@ugm.ac.id

Received:  15 July 2021; Accepted: 11 October 2021; Published:  xx October 2021

Abstract

# The use of eco-friendly natural dyes with lower environment impact is getting more interest. Indigo dye is one of the most popular natural dyes and has been used for textile dyeing since ages. The lower light fastness of natural indigo dye compared with blue synthetic dye has been a major disadvantage of its use in the textile industry. In this study, zinc oxide nanoparticles (ZnONPs) synthesized using simple precipitation method were applied as an anti-UV agent to protect the color of natural indigo dyed cotton. To increase the adsorption of ZnONPs in cotton, nanochitosan coating was applied before ZnONPs coating. X-ray diffraction (XRD) and transmission electron microscopy (TEM) were conducted to characterize the crystallinity, shape and size of the produced ZnO. The particle size distribution of ZnONPs and nanochitosan was measured using the dynamic light scattering technique. The amount of ZnO adsorbed in cotton, coated with and without nanochitosan were measured using energy-dispersive X-ray spectroscopy (EDS) and X-ray fluorescence (XRF). Applying nanochitosan coating before ZnONPs coating could increase the amount of ZnO adsorbed in cotton up to fourfold. The ability of ZnONPs as anti-UV agent to protect color of dyed cotton was measured by the photofading test. The photofading test was performed under UV-A light exposure and the color difference of cotton samples before and after 144 h irradiation was measured based on CIELAB value. Cotton dyed with natural indigo and coated with nanochitosan and ZnONP has a lowest color difference, indicating the increasing of light fastness provided by ZnONPs.

# Keywords:  zinc oxide nanoparticles, nanochitosan, natural indigo dye, adsorption, fading

# Abstrak

# Penggunaan pewarna asli dengan kesan yang lebih rendah terhadap alam sekitar semakin menarik dikembangkan. Pewarna indigo adalah salah satu pewarna asli yang popular dan telah digunakan untuk pewarnaan tekstil sejak zaman dahulu. Ketahanan cahaya pewarna indigo yang lebih rendah berbanding dengan pewarna sintetik telah menjadi kelemahan utama penggunaannya dalam industri tekstil. Dalam kajian ini, Zink oksida nanopartikel (ZnONPs) yang disintesis dengan kaedah pemendakan sederhana digunakan sebagai agen anti-UV untuk melindungi warna indigo pada kain kapas. Untuk meningkatkan penjerapan ZnONP, lapisan nano kitosan digunakan sebelum lapisan ZnONPs. Pembelauan sinar-X (XRD) dan mikroskop elektron transmisi (TEM) digunakan untuk mencirikan penghabluran, bentuk dan ukuran ZnO yang dihasilkan. Taburan ukuran zarah ZnONP dan nano kitosan diukur dengan teknik penyebaran cahaya dinamik (DLS). Jumlah ZnO yang diserap dalam kapas, dilapisi dengan dan tanpa nano-kitosan diukur menggunakan sinar-X pendafluoran (XRF). Salutan nano kitosan sebelum pelapisan ZnONP dapat meningkatkan jumlah ZnO yang diserap dalam kain kapas hingga empat kali. Ujian pudar dilakukan di bawah cahaya UV-A dan hasil sebelum dan setelah penyinaran selama 144 jam diukur dengan nilai CIELAB. Kain kapas yang diwarnai dengan indigo asli dan telah dilapisi nano-kitosan dan ZnONP mempunyai perbezaan warna yang paling rendah. Hal ini menunjukkan peningkatan daya tahan cahaya dapat disediakan oleh ZnONPs.

# Kata kunci:  zink oksida nanopartikel, nano-kitosan, indigo asli, jerapan, pudar

References

- Widiawati, D. (2009). The revival of the usage of natural fibers and natural dyes in Indonesian textile. ITB Journal of Visual Art and Design, 3(2): 115-128.

- Papanastasiou, M., Allen, N. S., McMahon, A., Naegel, L. C. A., Edge, M. and Protopappas, S. (2012). Analysis of indigo-type compounds in natural dyes by negative ion atmospheric pressure photoionization mass spectrometry. Dyes and Pigments, 92(3): 1192-1198.

- Padfield, T. and Landi, S. (1966). The light fastness of the natural dyes, Studies in Conservation, 11: 181-196.

- Saravanan, D. (2007). UV protection textile materials. Autex Research Journal, 7(1): 11-18.

- Fajzulin, I., Zhu, X. and Möller, M. (2015). Nanoparticulate inorganic UV absorbers: A review. Journal of Coatings Technology and Research, 12(4): 617-632.

- Schneider, S. L. and Lim, H. W. (2019). A review of inorganic UV filters zinc oxide and titanium dioxide. Photodermatology, Photoimmunology and Photomedicine, 35(6): 442-446.

- Becheri, A., Dürr, M., Lo Nostro, P. and Baglioni, P. (2008). Synthesis and characterization of zinc oxide nanoparticles: Application to textiles as UV-absorbers. Journal of Nanoparticle Research, 10(4): 679-689.

- Pulit-Prociak, J., Chwastowski, J., Kucharski, A. and Banach, M. (2016). functionalization of textiles with silver and zinc oxide nanoparticles. Applied Surface Science, 385: 543-553.

- Kathirvelu, S., D’Souza, L. and Dhurai, B. (2009). UV protection finishing of textiles using ZnO nanoparticles. Indian Journal of Fibre and Textile Research, 34(3): 267-273.

- Ibrahim, N. A., Eid, B. M., El-Aziz, E. A., Elmaaty, T. M. A. and Ramadan, S. M. (2017). Loading of chitosan–nano metal oxide hybrids onto cotton/polyester fabrics to impart permanent and effective multifunctions. International Journal of Biological Macromolecules, 105: 769-776.

- El-tahlawy, K. F., El-bendary, M. A., Elhendawy, A. G. and Hudson, S. M. (2005). The antimicrobial activity of cotton fabrics treated with different crosslinking agents and chitosan. Carbohydrate Polymers, 60: 421-430.

- Alonso, D., Gimeno, M., Olayo, R., Vázquez-Torres, H., Sepúlveda-Sánchez, J. D. and Shirai, K. (2009). Cross-linking chitosan into UV-irradiated cellulose fibers for the preparation of antimicrobial-finished textiles. Carbohydrate Polymers, 77(3): 536-543.

- Farouk, A., Moussa, S., Ulbricht, M. and Textor, T. (2012). ZnO nanoparticles-chitosan composite as antibacterial finish for textiles. International Journal of Carbohydrate Chemistry, 2012 (693629): 1-8.

- Raza, Z. A. and Anwar, F. (2016). Impregnation of zinc oxide mediated chitosan nano-composites on polyester fabric for performance characteristics. Fibers and Polymers, 17(9): 1378-1383.

- Preethi, S., Abarna, K., Nithyasri, M., Kishore, P., Deepika, K., Ranjithkumar, R., Bhuvaneshwari, V. and Bharathi, D. (2020). Synthesis and characterization of chitosan/zinc oxide nanocomposite for antibacterial activity onto cotton fabrics and dye degradation applications. International Journal of Biological Macromolecules, 164: 2779-2787.

- Abd Elhady, M.M. (2012). Preparation and characterization of chitosan/zinc oxide nanoparticles for imparting antimicrobial and UV protection to cotton fabric. International Journal of Carbohydrate Chemistry, 2012 (840591): 1-6.

- Tangkawanit, S. (2020). Color fastness and UV protection improvement of indigo dyed cotton fabrics coated with nano chitosan and zinc oxide. The Journal of King Mongkut’s University of Technology North Bangkok, 30(3): 1-13.

- Talam, S., Karumuri, S. R. and Gunnam, N. (2012). Synthesis, characterization, and spectroscopic properties of ZnO nanoparticles, ISRN Nanotechnology, 2012 (372505): 1-6.

- Liu, Z. R, Hou, J., Duan, L. M. and Xu, L. (2011). Study on the synthesis and properties of nano-ZnO, Materials Science Forum, 694: 324-327.

- Jo, M., Chung, H., Kim, H., Bae, S., Go, M., Yu, J. and Choi, S. (2016). Effects of zinc oxide nanoparticle dispersants on cytotoxicity and cellular uptake. Molecular and Cellular Toxicology, 12(3): 281-288.

- Tso, C. P, Zhung, C. M, Shih, Y.H, Tseng, Y., Wu, S.C. and Doong, R. A. (2010). Stability of metal oxide nanoparticles in aqueous solutions. Water Science and Technology, 61(1): 127-133.

- Rosyada, A., Sunarharum, W. B. and Waziiroh, A. (2019). Characterization of chitosan nanoparticles as an edible coating material. IOP Conference Series: Earth and Environmental Science, 230 (012043): 1-5.

- Turemen, M., Demir, A. and Gokce, Y. (2021). The synthesis and application of chitosan coated ZnO nanorods for multifunctional cotton fabrics. Materials Chemistry and Physics, 268(124736): 1-6.

- El.Shafei, A. and Abou-Okeil, A. (2011). ZnO/carboxymethyl chitosan bionano-composite to impart antibacterial and UV protection for cotton fabric. Carbohydrate Polymers, 83: 920-925.

- Ahmed, M. T., Sarhan, A. and Hassan, A. (2016). Preparation and characterization of ZnO nanoparticles by simple precipitation method. International Journal of Science, Engineering Technology, 4(3): 507-512.

- Wang, C., Lv, J., Ren, Y., Zhou, Q., Chen, J., Zhi, T., Lu, Z., Gao, D., Ma, Z. and Jin, L. (2016). Cotton fabric with plasma pretreatment and ZnO/carboxymethyl chitosan composite finishing for durable UV resistance and antibacterial property. Carbohydrate Polymers, 138: 106-113.

- Das, A., Sk., N. and Nair, R. G. (2019). Influence of surface morphology on photocatalytic performance of zinc oxide: A review, Nano-Structures and Nano-Objects, 19(100353): 1-18.