Malaysian Journal of Analytical Sciences Vol 26 No 1 (2022): 70 - 83

# SUPRAMOLECULAR ASSEMBLIES OF 1,2-DISUBSTITUTED CYCLOHEXANE AMIDE LIGANDS AND THEIR COORDINATION POLYMER: SYNTHESIS, CHARACTERISATION, AND

# CRYSTAL STRUCTURE

(Himpunan Supramolekul Ligan Amida Sikloheksana 1,2-Tertukar Ganti dan Polimer

Koordinatannya: Sintesis, Pencirian, dan Struktur Hablur)

# Nur Shuhaila Haryani Haris1, Nafisah Mansor1, Maisara Abdul Kadir1,2*

1Faculty of Science and Marine Environment,

2Advanced Nano Materials Research Group, Faculty of Science and Marine Environment,

Universiti Malaysia Terengganu, 21030 Kuala Nerus, Terengganu, Malaysia

# *Corresponding author:  maisara@umt.edu.my

Received:  13 September 2021; Accepted: 18 December 2021; Published:  xx February 2022

Abstract

Supramolecular interactions such as hydrogen bonding, π-π stacking, Van der Waals interactions, and metal-ligand are important in stabilising the structure of molecules. In order to determine the presence of supramolecular interactions in two novel compounds, 1,2-disubstituted cyclohexane amide ligands, namely 1,2-bis[N, N’-6-(3-pyridylmethylamido)pyridyl-2-carboxyamido]cyclohexane (L1) and 1,2-bis[N,N’-6-(4-pyridylmethylamido)pyridyl-2-carboxyamido]cyclohexane (L2) were successfully synthesised and fully characterised by FTIR, 1H and 13C NMR and mass spectrometry, while the molecular formula was determined by elemental analysis. X-ray crystallography revealed that the folded conformations of both ligands were stabilised by intramolecular N-H···O=C and N-H···N hydrogen bonds at the pre-organised amide moieties. The crystal’s structure was stabilised by weak face-to-face -stacking interaction or centroid-centroid -stacking interaction involving the two pendant pyridine rings. In the crystal structure of one-dimensional coordination polymer, there are two intermolecular hydrogen bonding interactions (N-H···O=C, d = 2.094 Å, D = 2.946 Å and d = 2.090 Å, D = 2.938 Å, N-H···O angle = 161.52) formed between the pre-organised NH amide donors of a molecule of L1 in one coordination polymer and the amide carbonyl group of a molecule of L1 in an adjacent polymer that leads to the formation of 2-D hydrogen-bonded sheets extend in the ac diagonal.

# Keywords:  supramolecular, coordination polymer, cyclohexane, hydrogen bonding, racemic

# Abstrak

Interaksi supramolekul seperti ikatan hidrogen, susunan π-π, interaksi Van der Waals dan logam-ligan adalah penting dalam menstabilkan struktur molekul. Dalam usaha mengenalpasti kehadiran interaksi supramolekul dalam dua sebatian baharu, ligan amida sikloheksana 1,2-tertukar ganti, iaitu 1,2-bis[N,N’-6-(3-piridilmetilamino)piridil-2-karboksiamido]sikloheksana (L1) and 1,2-bis[N,N’-6-(4-piridilmetilamido)piridil-2-karboksiamido]sikloheksana (L2) telah disintesis dan dicirikan sepenuhnya dengan FTIR, 1H dan 13C NMR serta spektrometri jisim, manakala formula molekul ditentukan melalui analisis unsur. Kristalografi sinar-X menunjukkan bahawa konformasi bagi kedua-dua ligan distabilkan oleh ikatan hidrogen intramolekul N-H···O=C dan N-H···N pada kawasan amida separa tersusun. Struktur hablur juga distabilkan oleh interaksi lemah susunan muka ke muka atau titik pusat ke titik pusat di antara gelang aromatik piridina. Dalam struktur hablur polimer koordinatan satu dimensi, terdapat dua ikatan hidrogen intermolekul (N-H···O=C, d = 2.094 Å, D = 2.946 Å dan d = 2.090 Å, D = 2.938 Å, N-H···O sudut = 161.52) yang terbentuk di antara NH amida dari molekul L1 dalam polimer koordinatan dan karbonil amida dari molekul L1 dalam polimer bersebelahannya dan menghasilkan lapisan 2-D ikatan hidrogen yang bersambung ke diagonal ac.

# Kata kunci:  supramolekul, polimer koordinatan, sikloheksana, ikatan hidrogen, rasemik

# References

- Lehn, J. M. (1988). Supramolecular chemistry-scope and perspectives molecules, supermolecules, and molecular devices (nobel lecture). Angewandte Chemie International Edition in English, 27(1): 89-112.

- Lu, R., Zhang, X., Cheng, X., Zhang, Y., Zan, X. and Zhang, L. (2020). Medical applications based on supramolecular self-assembled materials from tannic acid. Frontiers in Chemistry, 8: 1-25.

- Shuturminska, K., O'Malley, C., Collis, D. W. P., Conde, J. and Azevedo H.S. (2018). Displaying biofunctionality on materials through template self-assembly. Self-Assembling Biomaterials, 341-370.

- Qin, B., Yin, Z., Tang, X., Zhang, S., Wu, Y., Xu, J. F. and Zhang, X. (2020). Supramolecular polymer chemistry: From structural control to functional assembly. Progress in Polymer Science, 100: 101167.

- Deng, J. H., Luo, J., Mao, Y. L., Lai, S., Gong, Y. N., Zhong, D. C. and Lu, T. B. (2020). π- π Stacking interactions: Non-negligible forces for stabilizing porous supramolecular frameworks. Science Advances, 6(2): eaax9976.

- Frey, P. A. (2004). Low barrier hydrogen bonds. Encyclopedia of Biological Chemistry, 2004: 594-598.

- Wendler, K., Thar, J., Zahn, S. and Kirchner, B. (2010). Estimating the hydrogen bond energy. The Journal of Physical Chemistry A, 114: 9529-9536.

- Castiñeiras, A., Fernández-Hermida, N., García-Santos, I., Gómez-Rodríguez, L., Gil, D. M. and Frontera, A. (2021). Supramolecular, spectroscopic and computational analysis of weak interactions in some thiosemicarbazones derived from 5-acetylbarbituric acid. Journal of Molecular Structure, 5: 131031.

- Ghule, N. V., La, D. D., Bhosale, R. S., Kobaisi, M. A., Raynor, A. M., Bhosale, S. V. and Bhosale, S. V. (2016). Effect of amide hydrogen bonding interaction on supramolecular self-assembly of naphthalene diimideamphiphiles with aggregation induced emission. ChemistryOpen, 5(2): 157-163.

- Rong, X., Lin, H., Liu, D., Wang, X., Liu, G. and Wang X. (2016). Solvothermal synthesis, structures and properties of two new octamolybdate-based compounds with tetrazole- and pyridyl-containing asymmetric amide ligands. Inorganic Chemistry Communications, 71: 9-14.

- Haris, N. S. H., Mansor, N., Yusof, M. S. M., Sumby, C. J. and Kadir, M.A. (2021). Investigating the potential of flexible and pre-organized tetraamide ligands to encapsulate anions in one-dimensional coordination polymers: synthesis, spectroscopic studies and crystal structures. Crystals, 11: 77.

- Yusof, M. S. M., Ayob, N. A. C., Kadir, M. A. and Yamin, B. M. (2008). 1, 2-bis [N’-(2, 2-dimethylpropionyl) thioureido] cyclohexane. Acta Crystallographica Section E: Structure Reports Online, 64(5): o937.

- Shanmugharaj, A. M., Rhee, K. Y. and Ryu, S.H. (2006). Influence of dispersing medium on grafting of aminopropyltriethoxysilane in swelling clay materials. Journal of Colloid and Interface Science, 298(2): 854 -859.

- Oprea, S., Potolinca, V. O. and Varganici, C. D. (2016). Synthesis and properties of polyurethane urea with pyridine-2,6-dicarboxamide moieties in their structure. The Royal Society of Chemistry, 6(108): 106904–106913.

- Yalcin, S. P., Ceylan, U., Sarioglu, A. O. and Sonmez, M. (2015). Sythesis, structural, spectral (FT-IR, 1H and 13C NMR and UV-Vis), NBO and first order hyperpolarizability analysis of N-(4-nitrophenyl)-2, 2-dibenzoylacetamide by density functional theory. Journal of Molecular Structure, 1098: 400-407.

- Basak, A., Ghosh, S. C., Das, A. K. and Bertolasi, V. (2005). A novel azetidinyl γ-lactam based peptide with a preference for β-turn conformation. Organic and Biomolecular Chemistry, 3: 4050-4052

- Kushwaha, N., Saini, R. K. and Kushwaha, S. K. S. (2011). Synthesis of some amide derivatives and their biological activity. International Journal of ChemTech Research, 3(1): 203-209.

- Ikawa, T., Nishiyama, T., Shigeta, T., Mohri, S., Morita, S., Takayanagi, S-I., Terauchi, Y., Morikawa, Y., Takagi, A., Ishikawa, Y., Fujii, S., Kita, Y. and Akai, S. (2011). Ortho-selective nucleophilic addition of primary aminesto silylbenzynes: synthesis of 2-silylanilines. Angewandte Chemie, 123: 5792-5795.

- Hadadzadeh, H., Rezvani, A. R., Abdolmaleki, M. K., Ghasemi, K., Esfandiari, H. and Daryanavard, M. (2009). Pyridine-2,6-dicarboxylic acid (dipic): crystal structure from co-crystal to a mixed ligand nickel(II) complex. Journal of Chemical Crystallography, 40(1): 48-57.

- Kadir, M. A., Yusof, M. S. M., Sumby, C. J (2018). Conjoint experimental and theoretical evaluation of zinc (II) coordination polymer as potential anion receptors for nitrate and chromate. ASM Journal of Science, 1: 136-146.