Malaysian Journal of Analytical Sciences Vol 26 No 4 (2022): 819 - 828

# PRELIMINARY STUDIES ON SUNLIGHT ASSISTED DEGRADATION OF 2-CHLOROPHENOL USING MoS2/GO AS PHOTOCATALYST

(Kajian Awal Mengenai Cahaya Tampak Dituruti Penyusutan Sinaran 2-klorofenol Menggunakan MoS2/GO Sebagai Pemangkin Cahaya)

Kavirajaa Pandian Sambasevam, Syara Syazliana Muhammad Rajab, Izyan Najwa Mohd Norsham,

Siti Nor Atika Baharin*

Advanced Material for Environmental Remediation (AMER) Research Group, Faculty of Applied Sciences,

University Teknologi MARA, Cawangan Negeri Sembilan, Kampus Kuala Pilah,

72000, Kuala Pilah, Negeri Sembilan, Malaysia

*Corresponding author:  atikabaharin@uitm.edu.my

Received: 14 September 2021; Accepted: 24 March 2022; Published: xx August 2022

Abstract

This study highlighted preliminary studies on photodegradation of 2-chlorophenol using MoS2/rGO photocatalyst with different weight ratios under sunlight irradiation. The 2-chlorophenol is known as one of the most dangerous pollutant due to its hazardous properties of mutagenicity, carcinogenicity and eco-pollutant. The MoS2/rGO photocatalysts were synthesized using the hydrothermal method and used for the degradation of 2-chlorophenol under solar light irradiation. Three different compositions of MoS2/rGO (1%, 5% and 15%) were synthesized with different weight ratio of MoS2. The composites material of MoS2, GO and MoS2/rGO was characterized by FTIR and XRD indicating successful formation of MoS2/rGO composites. The photodegradation of the 10 ppm of 2-chlorophenol were observed under the exposure of sunlight for 180 minutes and analyzed using UV-VIS to measure percent degradation of 2-chlorophenol. 1% MoS2/rGO has been chosen as the composite to degrade 2-chlorophenol due to having the highest percent degradation of 51.41% among other photocatalysts.

Keywords: 	graphene oxide, molybdenum disulfide, photocatalytic degradation, semiconductor photocatalyst, solar irradiation

Abstrak

Kajian in menekankan kajian awal mengenai fotodegradasi 2-klorofenol dengan menggunakan berat ratio pemangkin cahaya MoS2/rGO yang berlainan dibawah radiasi matahari. 2-klorofenol dikenali sebagai salah satu bahan pencemar yang mempunyai ciri-ciri merbahaya seperti mutagenisiti, karsinogenik dan eko-pencemar. Komposit MoS2/rGO telah disintesis menggunakan kaedah hidroterma. Kaedah fotokatalisis yang menggunakan MoS2/rGO sebagai pemangkin cahaya untuk merosotkan 2-klorofenol dibawah sinaran matahari. Tiga komposisi MoS2/rGO yang berlainan (1%, 5% and 15%) telah disintesis menggunakan nisbah berat MoS2 yang berbeza. Bahan komposit MoS2, GO dan MoS2/rGO yang dicirikan menggunakan FTIR dan XRD telah menunjukkan hasil jaya pembentukan komposit MoS2/rGO dengan jayanya. Penyusutan sinaran oleh 10 ppm 2-klorofenol telah diperhatikan dibawah sinaran matahari selama 180 minit telah dianalisiskan dengan UV-VIS untuk mengukur peratus penyusutan sinaran 2-klorofenol. 1% MoS2/rGO telah dipilih untuk merosotkan 2-klorofenol kerana mempunyai peratusan penyosotan yang tinggi iaitu 51.41%.

Kata kunci: grafena oksida, molibdenum disulfida, degradasi fotokatalitik, pemangkin cahaya semikonduktor, penyinaran suria

References

- Li, K., Fang, X., Fu, Z., Yang, Y., Nabi, I., Feng, Y., Bacha, A. U. R. and Zhang, L. (2020). Boosting photocatalytic chlorophenols remediation with addition of sulfite and mechanism investigation by in-situ DRIFTs. Journal of Hazardous Materials, 398: 123007.

- Lei, M., Gao, Q., Zhou, K., Gogoi, P., Liu, J., Wang, J., Song, H., Wang, S. and Liu, X. (2021). Catalytic degradation and mineralization mechanism of 4-chlorophenol oxidized by phosphomolybdic acid/H2O2. Separation and Purification Technology, 257: 117933.

- Garba, Z. N., Zhou, W., Lawan, I., Xiao, W., Zhang, M., Wang, L., Chen, L. and Yuan, Z. (2019). An overview of chlorophenols as contaminants and their removal from wastewater by adsorption: A review. Journal of Environmental Management, 241: 59-75.

- Han, Z., Fei, J., Li, J., Deng, Y., Lv, M., Zhao, J., Wang, C. and Zhao, X. (2020). Enhanced dye-sensitized photocatalysis for water purification by an alveoli-like bilayer Janus membrane. Chemical Engineering Journal, 407: 127214.

- Abada, B., Alivio, T. E. G., Shao, Y., O’Loughlin, T. E., Klemashevich, C., Banerjee, S., Jayaraman, A.,     and Chu, K. H. (2018). Photodegradation of fluorotelomer carboxylic 5:3 acid and perfluorooctanoic acid using zinc oxide. Environmental Pollution, 243: 637-644.

- Elsalamony, R. A. and Mahmoud, S. A. (2017). Preparation of nanostructured ruthenium doped titania for the photocatalytic degradation of 2-chlorophenol under visible light. Arabian Journal of Chemistry, 10(2): 194-205.

- Soltani, T. and Lee, B. K. (2017). Enhanced formation of sulfate radicals by metal-doped BiFeO3 under visible light for improving photo-Fenton catalytic degradation of 2-chlorophenol. Chemical Engineering Journal, 313: 1258-1268.

- Barakat, M. A., Kumar, R. and Eniola, J. O. (2021). Adsorption and photocatalytic scavenging of 2-chlorophenol using carbon nitride-titania nanotubes based nanocomposite: Experimental data, kinetics and mechanism. Data in Brief, 34: 106664.

- Anjum, M., Oves, M., Kumar, R. and Barakat, M. A. (2017). Fabrication of ZnO-ZnS@polyaniline nanohybrid for enhanced photocatalytic degradation of 2-chlorophenol and microbial contaminants in wastewater. International Biodeterioration and Biodegradation, 119: 66-77.

- Onkani, S. P., Diagboya, P. N., Mtunzi, F. M., Klink, M. J., Olu-Owolabi, B. I. and Pakade, V. (2020). Comparative study of the photocatalytic degradation of 2–chlorophenol under UV irradiation using pristine and Ag-doped species of TiO2, ZnO and ZnS photocatalysts. Journal of Environmental Management, 260: 110145.

- Rueda-Marquez, J. J., Levchuk, I., Fernández Ibañez, P. and Sillanpää, M. (2020). A critical review on application of photocatalysis for toxicity reduction of real wastewaters. Journal of Cleaner Production, 258: 120694

- Prasad, C., Liu, Q., Tang, H., Yuvaraja, G., Long, J., Rammohan, A. and Zyryanov, G. V. (2020). An overview of graphene oxide supported semiconductors based photocatalysts: Properties, synthesis and photocatalytic applications. Journal of Molecular Liquids, 297: 111826.

- Chen, Y., Zhai, B. and Liang, Y. (2019). Enhanced degradation performance of organic dyes removal by semiconductor/MOF/graphene oxide composites under visible light irradiation. Diamond and Related Materials, 98: 107508.

- Kamalam, M. B. R., Inbanathan, S. S. R. and Sethuraman, K. (2018). Enhanced photo catalytic activity of graphene oxide /MoO3 nanocomposites in the degradation of Victoria Blue Dye under visible light irradiation. Applied Surface Science, 449: 685-696.

- Cao, Y., Wang, P., Fan, J. and Yu, H. (2021). Covalently functionalized graphene by thiourea for enhancing H2-evolution performance of TiO2 photocatalyst. Ceramics International, 47(1): 654-661.

- El-Fawal, E. M., Younis, S. A. and Zaki, T. (2020). Designing AgFeO2-graphene/Cu2(BTC)3 MOF heterojunction photocatalysts for enhanced treatment of pharmaceutical wastewater under sunlight. Journal of Photochemistry and Photobiology A: Chemistry, 401: 112746.

- Long, D., Peng, J., Liu, H., Feng, Z., Chen, L., Chen, X. and Lu, M. (2020). Graphene oxide discarded solution for high surface area photocatalyst. Solar Energy Materials and Solar Cells, 209: 110446.

- Asaithambi, S., Sakthivel, P., Karuppaiah, M., Balamurugan, K., Yuvakkumar, R., Thambidurai, M. and Ravi, G. (2021). Synthesis and characterization of various transition metals doped SnO2@MoS2 composites for supercapacitor and photocatalytic applications. Journal of Alloys and Compounds, 853: 157060.

- Yu-Cheng, C. and Yu-Wen, L. (2020). MoS2@SnO2 core-shell sub-microspheres for high efficient visible-light photodegradation and photocatalytic hydrogen production. Materials Research Bulletin, 129: 110902.

- Zhao, Y., Zhang, X., Wang, C., Zhao, Y., Zhou, H., Li, J. and Jin, H. B. (2017). The synthesis of hierarchical nanostructured MoS2 /Graphene composites with enhanced visible-light photo-degradation property. Applied Surface Science, 412: 207-213.

- Rani, A., Singh, K., Patel, A. S., Chakraborti, A., Kumar, S., Ghosh, K. and Sharma, P. (2020). Visible light driven photocatalysis of organic dyes using SnO2 decorated MoS2 nanocomposites. Chemical Physics Letters, 738: 136874.

- Zaaba, N. I., Foo, K. L., Hashim, U., Tan, S. J., Liu, W. W. and Voon, C. H. (2017). Synthesis of graphene oxide using modified hummers method: solvent influence. Procedia Engineering, 184: 469-477.

- Gopalakrishnan, K., Sultan, S., Govindaraj, A. and Rao, C. N. R. (2015). Supercapacitors based on composites of PANI with nanosheets of nitrogen-doped RGO, BC1.5N, MoS2 and WS2. Nano Energy, 12: 52-58.

- Song, Y., Cao, K., Li, W., Ma, C., Qiao, X., Li, H. and Hong, C. (2020). Optimal film thickness of rGO/MoS2 @ polyaniline nanosheets of 3D arrays for carcinoembryonic antigen high sensitivity detection. Microchemical Journal, 155: 104694.

- Hanafi, N. N., Sambasevam, K. P., Arifutzzaman, A., Rahman, S. and Baharin, S. N. A. (2020). Solar-driven degradation of 2-chlorophenol using PANI/GO as photocatalyst. Orbital, 12(4): 205-212.

- Pawson, S. (n.d.). Weatherspark.com. Average Weather in April in Kuala Pilah, Malaysia - Weather Spark. https://weatherspark.com/m/ 114181/4/Average-Weather-in-April-in-Kuala-Pilah-Malaysia.

- Phung, H. N. T., Truong, N. D., Duong, P. A. and Tuan Hung, L. V. (2018). Influence of MoS2 deposition time on the photocatalytic activity of MoS2/ V, N co-doped TiO2 heterostructure thin film in the visible light region. Current Applied Physics, 18(6): 737-743.

- Chao, J., Yang, L., Zhang, H., Liu, J., Hu, R. and Zhu, M. (2020). Engineering layer structure of MoS2/polyaniline/graphene nanocomposites to achieve fast and reversible lithium storage for high energy density aqueous lithium-ion capacitors. Journal of Power Sources, 450: 227680.

- Beura, R., Pachaiappan, R. and Paramasivam, T. (2021). Photocatalytic degradation studies of organic dyes over novel Ag-loaded ZnO-graphene hybrid nanocomposites. Journal of Physics and Chemistry of Solids, 148: 109689.

- Saha, S., Chaudhary, N., Mittal, H., Gupta, G. and Khanuja, M. (2019). Inorganic–organic nanohybrid of MoS2-PANI for advanced photocatalytic application. International Nano Letters, 9(2): 127-139.

- Sha, C., Lu, B., Mao, H., Cheng, J., Pan, X., Lu, J. and Ye, Z. (2016). 3D ternary nanocomposites of molybdenum disulfide/polyaniline/reduced graphene oxide aerogel for high performance supercapacitors. Carbon, 99: 26-34.